Bandwidth Control for Photonic Bandgap Waveguides

A. Boag1, M. Gafni2, and B. Z. Steinberg2

1	Faculty of Engineering, Department of Physical Electronics, Tel Aviv University,

Tel Aviv 69978, Israel

Fax: + 972-3-6423508; E-mail: boag@eng.tau.ac.il

2	Faculty of Engineering, Department of Interdisciplinary Studies, Tel Aviv University,

Tel Aviv 69978, Israel

E-mail: steinber@eng.tau.ac.il

##### Abstract

A widely spaced periodic array of defects in the photonic band gap crystal is studied with the goal of designing a waveguide with a prescribed narrow bandwidth. Tunnelling of radiation between the defect sites allows wave propagation along the line of the defects. A design procedure based on the weakly coupled cavity model is proposed. The frequency shift and the band structure of the periodic defect waveguide are linked by an analytic relationship to the distance between the defect sites and therefore can be tuned by varying the latter. Sections of such waveguides can be employed as ultra narrow band filters in optical routing devices.

1.	Introduction

Photonic band gap materials attracted much attention in the context of designing optical and microwave devices. Recently numerical experiments have shown that line defects in photonic crystals can be used not only to guide but also to multiplex and demultiplex optical signals [1]. Most researchers studying the wave guiding by line defects employ photonic band waveguides obtained by removal or modification of consecutive posts in the periodic structure. The strong coupling between the adjacent defects produces relatively wideband waveguides.

In this paper, we address the issue of designing photonic bandgap waveguides with a prescribed narrow bandwidth.  Specifically, we concentrate on a problem of a waveguide formed by widely spaced periodic defects in the photonic band gap crystal. Tunnelling of radiation between the defect sites allows wave propagation along the line of defects. Sections of such waveguides can be employed as ultra narrow band filters in optical routing devices. Here, we propose a design procedure based on the weakly coupled cavity model. This approach resembles the tight binding perturbation theory of the solid-state physics. A single defect mode with a resonant frequency in the band gap is analyzed first. Coupling between the periodic defects causes a discrete spectral line to turn into a narrow band of guided frequencies shifted from the original frequency of a single defect. The perturbation theory facilitates an approximate calculation of both the frequency shift and the band structure of the periodic defect waveguide. Furthermore, these parameters are linked by an analytic relationship to the distance between the defect sites. Consequently, the latter distance can be directly tuned to achieve the desirable waveguide properties. The design results are verified by a comparison with numerically rigorous computations employing the current model technique [2].

2.	Formulation

Consider a problem of designing a narrow band waveguide formed by widely spaced periodic defects in the photonic band gap crystal. The time harmonic electromagnetic problem in an inhomogeneous dielectric can be cast in an eigenvalue form for the magnetic field H [3]:

(1)

where  is the frequency, c is the free space speed of light, and  denotes a Hermitian operator defined by

(2)

In (2),  denotes the relative permittivity. Alternatively, the eigen-frequencies can be expressed in the variational form:

(3)

where  denote the inner product defined by

(4)

The unperturbed crystal is characterized by a periodic relative permittivity .  First, consider a single defect within the periodic structure arbitrarily centered at the origin of the coordinate system. The localized defect can be characterized by the change in the reciprocal permittivity , where  denotes the permittivity of the photonic crystal with a single defect. We assume that this defect allows for a localized mode with a frequency  falling in the band gap of the unperturbed crystal.   Specifically by analogy to (1),

(5)

is the operator of the periodic structure  and  is the defect operator. The operators  and  are defined by analogy to (2) via replacing  by  and , respectively.

Now, we turn to the case of a linear array of defects obtained by a periodic repetition of the defect. The reciprocal permittivity of the photonic crystal with the linear array of non-overlapping defects is given by

(6)

where the vector b is assumed to be an integral multiple of the lattice vector a, , .  The operator ,

(7)

which comprises a superposition of  and shifted operators  defined by analogy with (2) via replacing  by  for .

Following the strong binding perturbation theory [4] for the linear array, we seek a modal solution of the form

(8)

where  and  is a set of yet to be determined coefficients.  Substitution of (7) and (8) in (3) yields

(9)

where

(10)

and

(11)

Note that due to the periodicity of the array the integrals in (10) and (11) depend only on n-m. According to variational principle the frequency expressed by (9) is stationary with respect to the coefficients . We have

(12)

Discrete shift invariant nature of (12) suggest that modal solution of the form  whose use in (12) yields

(13)

Using (5), we have

(14)

where

(15)

Substituting (14) in (13) we obtain

(16)

namely, an expression for the frequency shift of the linear array mode with wavenumber k/b relative to the frequency of the localized mode. For sufficiently spaced defects we can make the first order approximation by retaining only the nearest neighbor interactions. Specifically, we have  and . On the other hand,  and  can be comparable in magnitude.  With this approximations and assuming  we obtain

(17)

The total bandwidth of the waveguide formed by the periodic array for propagating modes  is given by

(18)

Furthermore due to weak coupling and Hermitian property of ,

(19)

Once the localized modal solution is known, equations (18)-(19) allow for straightforward estimation of the waveguide bandwidth for various spacings between defects, . Note that in (19),  and  is a local operator. For sufficiently large , the localized magnetic field  is decaying exponentially away from the origin. Thus, (19) indicates that increasing  can reduce the waveguide bandwidth. The bandwidth control by varying defect spacing will be demonstrated via numerical examples.

References

[1]	E. Centeno, B. Guizal, and D. Felbacq, J. Opt. A.: Pure Appl. Opt., No. 1, pp. L10-L13, 1999.

[2]	A. Boag, Y. Leviatan, and A. Boag, Radio Science, Vol. 23, pp. 612-624, 1988.

[3]	J. D. Joannopoulos, R. D. Meade, and J. N. Winn, Photonic Crystals: Molding the Flow of Light. Princeton University Press, 1995.

[4]	R. E. Peierls, Quantum Theory of Solids. Oxford Clarendon Press.