Reconstruction of the Constitutive Parameters

for Composite Media

Using Kramers - Kronig Analysis

A. O. Pinchuk

Institute of Surface Chemistry

National Academy of Science of Ukraine

Kyiv, Nauki av., 31,  Ukraine, 03022

Fax: (380) 44 264 04 46, e-mail: onmf@serv.biph.kiev.ua

Abstract

An alternative method of determining of the constitutive dispersion parameters for composite media is discussed. It is assumed, that the constitutive materials of composite media are characterized by the complex dielectric permittivity. Furthermore, we consider the composite media with small inclusions as compared with the wavelength of that range for which the dispersion parameters are determined. We have used the experimental reflectance spectra of the composite media from which the effective complex optical refractive index and effective complex dielectric permittivity were determined.

1.	Introduction

Last time considerable attention has been devoted on the inverse problem of determining the constitutive parameters of complex media [1-3]. Sometimes using of general methods for determining the constitutive parameters of such media, e.g. solutions of biological macromolecules in aqueous media, is restricted by strong absorption of water outside the transparent ranges. To overcome this problem an alternative method of Kramers-Kroning analysis of the experimental spectra can be applied [3]. In this work, the effective optical functions nand k, were obtained using Kramers-Kroning analysis from the experimental reflectance spectra of the composite medium. The real and imaginary parts of the effective complex dielectric permittivity ε were calculated using the effective optical functions.

- Theory

The complex reflection amplitude of a normal incident electromagnetic wave, used in the Kramers-Kronig analysis, is defined as follows [1]

R12=(n−1)+ik(n+1)+ik=R12eiϕ	(1)

were R is the magnitude of the reflectance at the frequency ω. The phase  is related to the reflectance by the dispersion equation, defined in the Kramers-Kronig analysis as follows

ϕ(ω)=ωπP0∞lnR(ξ)ξ2−ω2dξ−π	(2)

were P stands for the Cauchy principal value. The real and imaginary parts of the complex optical refractive index nand kare related  to the reflectance amplitude and phase by the relations

n=1−R1+R+2R12cosϕ,        {k=−2R12sinϕ1+R+2R12cosϕ	(3)

Using obtained complex refractive index we can calculate the real and imaginary parts of the effective dielectric permittivity of the composite mediumε1=n2−k2,ε2=2nk. Further, using the effective complex permittivity of the composite medium, we can obtain the complex dielectric permittivity of the constituents. For this purpose we can utilize one of the widely used approximations, such as Maxwell-Garnett or Bruggeman formalism

εMG=εh+3fεhεi−εh(1−f)εi+(2+f)εh ,  fεi−εBGεi+2εBG+(1−f)εh−εBGεh+2ε=0	(4)

were εiis the dielectric permittivity of the inclusions, εh is the dielectric permittivity of the host medium. Using known dielectric parameters of the host and the filling factor for the inclusions, we can reconstruct the dielectric permittivity for the inclusions, or using known dielectric permittivity of the inclusions and host medium we can determine the filling factor of the inclusions.

- Numerical results

To demonstrate the validity of the above formalism the composite structure was considered in a mixture form of LiF small particles embedded in a KBr host. The optical constants for LiF particles correspond to the classical oscillator theory. The relevant real and imaginary parts of the complex dielectric permittivity have the following form

ε'=n2−k2=ε∞+j4πρjωj2ωj2−ω2ωj2−ω22+γjωj2, ε''=2nk=j4πρjωj2γjωjωj2−ω22+γjωj2	(5)

The experimental reflectance spectra, taken from the literature [5], for the composite structure with filling factor f=0.2 is shown on Fig.1. The calculated phase using Kramers-Kroning analysis is shown on same Fig.1. The effective optical constants of LiF-KCl composite, calculated using Kramers-Kroning, are shown on Fig.2. The experimental and restored effective complex dielectric permittivity for LiF-KCl composite are shown on Fig.3. Finaly, the restored real and imaginary parts of the complex dielectric permittivity of the inclusions are shown on Fig. 4.

- Conclusion

The apparent conformity of restored complex effective dielectric permittivity with experimental curves proves the validity of above formalism. This rather simple procedure will be useful for spectroscopic investigation of complex media, e.g. in spectroscopic studying of biological macromolecules immersed in aqueous solutions with known dispersion properties.

References

[1]	C. F. Bohren and D. R. Huffman, Absorption and Scattering of Light by Small Particles, New York, Wiley Publisher, 1983.

[2]	Martin Norgren and Sailing He, "Reconstruction of the Constitutive Parameters for an Ω Material in a Rectangular Waveguide," JEEE Trans. On Microwave Theory and Techniques,  vol. 43, no. 6, pp. 1315-1321,  June 1995.

[3]	J. M. Heller, R. N. Hamm, R. D. Bikhoff, and L. R. Painter, "Collective oscillation in liquid water," The Journal of Chemical Physics, vol. 60, no. 9, pp. 3483-3486, May 1974.

[4]	J. R. Jasperse, A. Kahan, and J. N. Plendl, Phys. Rev. vol. 146 , pp. 526-542, 1966.

Fig 1 Reflectance spectra and restored faze of reflected wave for LiF particles embedded in KBr host.

Fig. 2 Restored real and imaginary parts for the effective dielectric permittivity.

Fig. 3  Restored real and imaginary parts of the complex effective optical functions

.

Fig. 4  Restored real and imaginary parts of the dielectric permittivity of the inclusions.